SECTION 10 2113

TOILET COMPARTMENTS

PART 1- GENERAL

1.1 	SUMMARY

A.	This Section includes Paper Composite Units as follows:

1. Toilet Enclosures: Floor mounted/overhead braced

2. Urinal Screens: Wall hung

1.2 	SUBMITTALS

A.	Product Data: Provide data on panel construction and hardware.

B. 	Shop Drawings:

1. Plans

2. Elevations

3. Sections & details

4. Attachments to other work.

C.	Samples for Verification: Include minimum 3” squares of each type of color and finish         	required for units.

1.3 	COORDINATION

A. 	Coordinate the work with placement of support framing and blocking in walls.

  - QUALITY ASSURANCE

Consider retaining first paragraph below for Federal projects.

Retain first paragraph below if Owner or authorities having jurisdiction require that toilet compartments made of combustible materials comply with surface-burning requirements.  Metal units are inherently noncombustible.  Flame-spread index options correspond to flame-spread and smoke-developed Classes A, B, and C; verify, with manufacturers selected, availability of suitable units.  See "Fire-Test-Response Characteristics" Article in the Evaluations.

Regulatory Requirements:  Comply with applicable provisions in the U.S. Architectural & Transportation Barriers Compliance Board's "Americans with Disabilities Act (ADA) and Architectural Barriers Act (ABA) Accessibility Guidelines for Buildings and Facilities" and ICC/ANSI A117.1 for toilet compartments designated as accessible.

Warranty: 15-year, limited commercial warranty.

PART 2- PRODUCTS

2.1 	MANUFACTURERS

A.	Toilet compartments and urinal screens to be manufactured by Surfaces group, LLC, (866) 896-1127 | www.surfacesgroup.com

1.	Partition system: Eco-Screen Privacy Compartments and Urinal Screens

2.	Color: To be selected from Manufacturer’s full color range

  - COMPONENTS

        - Toilet compartments: Phenolic composite panels, doors and pilasters; floor mounted, 	head rail braced.

1.	Product: PaperStone distributed by North Star Surfaces LLC: 					www.nssurfaces.com.

2. 	Composition: 100 percent post-consumer recycled paper and water-based 			petroleum free phenolic resin; emits no volatile organic compounds (VOC’s) or 			formaldehyde.

3. 	Surface Characteristics: Manufactured surface normally includes some tonal 			variation, striations, mottling and slight variation/unevenness.

4. 	Combustibility: Comply with ASTM E84; Class A, UBC Class II, flame spread 			20 / smoke density 110.

        - Door and Panel Dimension:

Nominal Thickness/Minimal:

Doors: ¾ inch (19mm)

Panels ¾ inch (19 mm)

Door width 24 inches nominal (610mm)

Door  width for handicap use: minimum 34” (864mm)

Height: 58 inches (1475mm)

Pilaster Thickness: Nominal ¾ inch (19mm)

D.	Urinal Screens : Nominal ¾ inch (19mm). Size (WxH) 18 inch by 42 inch (457mm x 1066mm)

2.3 	ACCESSORIES

A.	Hardware and Accessories: Manufacturer's standard design, heavy-duty operating hardware and accessories.

B.	Overhead Bracing: (To be selected)

1. 	Manufacturer's continuous Aluminum head rail with anti-grip profile and in manufacturer’s standard finish.

2.	Manufacturer's continuous PaperStone head rail with anti-grip profile and in manufacturer’s standard finish.

3.	Manufacturer's continuous Decorative Curved PaperStone head rail, with anti-grip profile and in manufacturer's standard finish.

C.	Support Posts for Urinal Screens: Manufacturer's standard double ear extruded aluminum continuous bracket.

D. 	Anchorages and Fasteners: Manufacturer's standard exposed fasteners of stainless steel, finished to match hardware, with theft-resistant-type heads. Provide sex-type bolts for through-bolt applications.  For concealed anchors, use hot-dip galvanized, or other rust-resistant, protective-coated steel.

2.4 	FABRICATION

- Perform as per manufacturers instructions and approved shop drawings.

- Fabricate doors, panels and pilasters from full sheets avoiding having seams in completed units.

- Sand panels in accordance with manufacturers recommendations

- Apply final treatment of proprietary panel finish in accordance with manufacturers recommendations.

PART 3 - EXECUTION

3.1 	INSTALLATION

A.	General: Manufacturer to provide written installation instructions. Install units rigid, straight, level, and plumb. Secure units in position with manufacturer's recommended anchoring devices.

1.	Maximum Clearances:

a.	Pilasters and Panels: 1/2 inch (13 mm).

b.	Panels and Walls: 1 inch (25 mm).

2.	Brackets: Secure panels to walls and to pilasters with continuous angle or U-brackets as indicated in the shop drawings.

B. 	Secure pilasters to floor and level, plumb, and tighten. Secure continuous head rail to each pilaster with not less than two fasteners. Hang doors to align tops of doors with tops of panels and adjust so tops of doors are parallel with overhead brace when doors are in closed position.

C.	Wall-Hung Urinal Screens: Attach with anchoring devices as detailed in the shop drawings. Set units level and plumb, and to resist lateral impact.

3.2 	ADJUSTING

- Hardware Adjustment: Adjust hardware according to manufacturer's written instructions for proper operation. Set hinges on in-swinging doors to hold doors open approximately 30 degrees from closed position when unlatched. Set hinges on out-swinging doors to return doors to fully closed position.

END OF SECTION 10 2113